Additive manufacturing powders are available in the following stock sizes. If you need to have it customized to your requirements, please indicate the size distribution. They can be tailored to your needs.

- 0-45 microns

- 0-53 microns

- 15-45 microns

- 15-53 microns

- 45-150 microns

| Product | Composition | Chemical Compositions (wt.%) |
| --- | --- | --- |
| Cobalt Base | CoCrMo alloy powder | Co: Bal. | Cr: 26.6-30 |
|  |  | Mo: 4.5-7.0 | Mn: ≤1.0 |
|  |  | Fe: ≤1.0 | Ni: ≤1.0 |
|  |  | Si: ≤1.0 | C: ≤0.35 |
|  | CoCrMoW alloy powder | Co: Bal. | Cr: 23.7-25.7 |
|  |  | W: 4.9-5.9 | Mo: 4.6-5.6 |
|  |  | Si: 0.8-1.2 | Fe: ≤0.5 |
|  |  | Mn: ≤1.0 |  |
|  | CoCrW alloy powder | Cr:26-30 | W:7.5-9.5 |
|  |  | Si:0.65-2.65 | Mn:≤0.5 |
|  |  | Fe:≤0.5 | Co:Bal. |
|  |  | Be:≤0.01 | Cd:≤0.01 |
|  |  | Ni:≤0.1 |  |
| Iron Base | 15-5PH stainless steel powder | C: ≤0.07 | Si: ≤1.0 |
|  |  | Mn: ≤1.0 | P: ≤0.04 |
|  |  | S: ≤0.03 | Ni: 3.5-5.5 |
|  |  | Cr: 14.0-15.5 | Cu: 2.5-4.5 |
|  |  | Nb: 0.15-0.45 | Fe: Bal. |
|  | 17-4PH stainless steel powder | Fe: Bal. | Ni: 3.0-5.0 |
|  |  | Cr: 15.0-17.0 | Cu: 3.0-5.0 |
|  |  | Nb: 0.15-0.45 | Mn: ≤1.0 |
|  |  | Si: ≤1.0 |  |
|  | 18Ni300 steel powder | Fe: Bal. | Ni: 17.0-19.0 |
|  |  | Mo: 4.5-5.2 | Co: 8.5-9.5 |
|  |  | Ti: 0.6-0.8 | Al: 0.05-0.15 |
|  |  | Cr: ≤0.3 | Mn: ≤0.1 |
|  | 316L stainless steel powder | Fe: Bal. | Mo: 2.0-3.0 |
|  |  | Cr: 16.0-18.0 | Ni: 10.0-14.0 |
|  |  | Mn: ≤2.0 | Si: ≤1.0 |
| Nickel Base | GH3536 superalloy powder | Ni: Bal. | Mo: 8.0-10.0 |
|  |  | Cr: 20.5-23 | Fe: 17-20 |
|  |  | Co: 0.5-2.5 | W: 0.2-1.0 |
|  |  | C: 0.05-0.15 | Ti: ≤0.15 |
|  |  | Si: ≤1.0 | P: ≤0.25 |
|  |  | Cu: ≤0.5 | Mn: ≤1.0 |
|  |  | Al: ≤0.5 |  |
|  | GH3625 superalloy powder | Fe: ≤5.0 | S: ≤0.015 |
|  |  | P: ≤0.015 | Nb: 3.15-4.15 |
|  |  | Ti: ≤0.4 | Cu: ≤0.07 |
|  |  | Al: ≤0.4 | Mo: 8.0-10.0 |
|  |  | Co: ≤1.0 | Cr: 20.0-23.0 |
|  |  | Ni: Bal. | Mn: ≤0.5 |
|  |  | Si: ≤0.5 | C: ≤1.0 |
|  | GH4099 superalloy powder | C: ≤0.08 | Cr: 17-20 |
|  |  | Ni: Bal. | W: 5.0-7.0 |
|  |  | Mo: 3.5-4.5 | Al: 1.7-2.4 |
|  |  | Co: 5.0-8.0 | Ti: 1.0-1.5 |
|  |  | Fe: ≤2.0 | B: ≤0.05 |
|  |  | Mg: ≤0.01 | Ce: ≤0.02 |
|  |  | Mn: ≤0.4 | Si: ≤0.5 |
|  |  | P: ≤0.015 | S: ≤0.015 |
|  | K418 superalloy powder | C: 0.08-0.16 | Cr: 11.5-13.5 |
|  |  | Ni: Bal. | Mo: 3.8-4.8 |
|  |  | Al: 5.5-6.4 | Ti: 0.5-1.0 |
|  |  | Fe: ≤1.0 | Nb: 1.8-2.5 |
|  |  | B: 0.008-0.02 | Zr: 0.06-0.15 |
|  |  | Mn: ≤0.5 | Si: ≤0.5 |
|  |  | P: ≤0.015 | S: ≤0.01 |
|  |  | Pb: ≤0.0005 | Sb: ≤0.001 |
|  |  | As: ≤0.001 | Sn: ≤0.001 |
|  |  | Bi: ≤0.00005 |  |
|  | K438 superalloy powder | C: 0.1-0.2 | Si: ≤0.3 |
|  |  | Mn: ≤0.2 | P: ≤0.015 |
|  |  | S: ≤0.015 | Cr: 15.7-16.3 |
|  |  | Ni: Bal. | Mo: 1.5-2.0 |
|  |  | Co: 8.0-9.0 | Ta: 1.5-2.0 |
|  |  | Fe: ≤0.5 | Nb: 0.6-1.1 |
|  |  | B: 0.05-0.015 | Ti: 3.0-3.5 |
|  |  | Al: 3.2-3.7 | Zr: 0.05-0.15 |
|  |  | W: 2.4-2.8 |  |
|  | K477 superalloy powder | C: 0.05-0.09 | Cr: 14.0-15.25 |
|  |  | Mo: 3.9-4.5 | Ni: Bal. |
|  |  | Co: 14.0-16.0 | Al: 4.0-4.6 |
|  |  | Ti: 3.0-3.7 | Fe: ≤1.0 |
|  |  | Si: ≤0.5 | Mn: ≤0.2 |
|  |  | P: ≤0.015 | S: ≤0.01 |
|  |  | B: 0.012-0.02 | Zr: ≤0.04 |
|  |  | Ce: ≤0.1 |  |
| Titanium Base | NiTi Shape memory alloy powder | Ni: 50.1-55.0 | Ti: Bal. |
|  | TA0 Commercially pure titanium powder | Fe: ≤0.2 | C: ≤0.08 |
|  |  | H: ≤0.015 | Si: Bal. |
|  |  | Al: 20.0-23.0 | V: ≤1.0 |
|  |  | Mo: 8.0-10.0 | Sn: ≤0.4 |
|  |  | Ti: ≤0.4 |  |
|  | TA15 Titanium alloy powder | Ti: Bal. | Al: 5.5-7.1 |
|  |  | V: 0.8-2.5 | Zr: 1.5-2.5 |
|  |  | Mo: 0.5-2.0 | Si: ≤0.15 |
|  | TC11 Titanium alloy powder | Al: 5.8-7.0 | Mo: 2.8-3.8 |
|  |  | Zr: 0.8-2.0 | Si: 0.2-0.35 |
|  |  | Ti: Bal. | Fe: ≤0.25 |
|  |  | C: ≤0.08 | N: ≤0.05 |
|  |  | H: ≤0.012 | O: ≤0.15 |
|  | TC4 Titanium alloy powder | Ti: Bal. | Al: 5.5-6.75 |
|  |  | V: 3.5-4.5 | Fe: ≤0.3 |
| Tantalum powder, spherical | Class 1 | 99.8% min | <10 microns |
|  | Class 2 | 99.8% min | 10-50 microns |
|  | Class 3 | 99.8% min | 50-150 microns |
| Titanium powder, spherical | Class 1 | 99.5% min | 0-15 microns |
|  | Class 2 | 99.5% min | 15-53 microns |
|  | Class 3 | 99.5% min | 45-150 microns |
| Tungsten powder, spherical | Class 1 | 99.95% | 0-15 microns |
|  | Class 2 | 99.95% | 15-53 microns |
|  | Class 3 | 99.95% | 45-150 microns |
| Tungsten carbide, cobalt binder | Class 1 |  | 0-15 microns |
|  | Class 2 |  | 15-53 microns |
|  | Class 3 |  | 45-150 microns |
| Molybdenum powder, spherical | Class 1 | 99.8% min | 0-15 microns |
|  | Class 2 | 99.8% min | 15-53 microns |
|  | Class 3 | 99.8% min | 53-150 microns |