Technical Data Sheet

Amorphous Boron Powder

MIL-B-51092

PRODUCT INFORMATION

Amorphous Boron Powder –   	requires an export license

CAS Number:	7440-42-8

RTECS Number:	ED 7350000

Melting Point:	~2200 °C

Density:	2.350

EINEC Number:	2311512

Molecular Weight:	10.8

Molecular Formula:	B

Water Solubility:	Insoluble

TYPICAL CHEMICAL ANALYSIS

Catalog No.:  	MIL-B-51092	MIL-B-51092

Total Boron: 	95% Min. 	90.0% Min.

Water Soluble Boron: 	0.2% Max. 	0.5% Max.

H2O2 Insoluble: 	1.0% Max. 	1.0% Max.

Moisture: 	0.5% Max 	0.5% Max.

Oxygen: 	2.2% Max. 	4.5% Max.

Nitrogen: 	0.4% Max. 	0.3% Max.

Magnesium: 	0.8% Max. 	6.0% Max.

Average Particle Size*:    	1.0 μ Max.* 	0.8 μ Max.*

Specific Surface Area: 	10.0 m2/g 	18.0 m2/g

* Method Fisher Sub Sieve (FSSS) per ASTM B330

USES:	Boron is used as an oxygen scavenger for copper and other metals.  It is used in manufacturing alloys usually to harden other metals.  In nuclear chemistry, boron is used as a neutron absorber.  In pyrotechnic chemistry, boron is used in ignition formulations, rocket-propellant mixtures, and other burn control formulations.

HANDLING:	Avoid contact with skin and avoid ingestion.  Use dust respirator when handling.  Since no exposure limits have been established for Boron by OSHA & ACGIH, we recommend that our product should be treated as a nuisance dust 15 mg/m3.  Avoid dusting of Boron because it can spontaneously ignite in air.  See MSDS for more information.

PROPER SHIPPING NAME:	Boron Powder (Amorphous)

& SHIPPING INFORMATION:	No Label Required

Although the information and recommendations set forth herein (hereinafter “Information”) are presented in good faith and believed to be correct as of the date hereof, Atlantic Equipment Engineers makes no representations as to the completeness or accuracy thereof. Information is supplied upon the condition that the persons receiving same will make their own determination as to its suitability for their purposes prior to use.  In no event will Atlantic Equipment Engineers be responsible for damages of any nature whatsoever resulting from the use of or reliance upon Information.

No representations or warranties either express or implied, of merchantability, fitness for a particular purpose, that the products to which the information refers may be used without infringing the intellectual property rights of others, or of any other nature are made hereunder with respect to information or the product to which information refers. In no case shall the information be considered a part of our terms and conditions of sale.