ALUMINUM POWDER, FLAKED GRAINED, AND ATOMIZED

MIL-DTL-512D

23 March 18

Superseding

MIL-DTL-512C

3 December 01

Classification

| Type | Grade | Class |
| --- | --- | --- |
| Type I – Flaked | A | 1 |
|  | B | 2 |
|  |  | 2A |
|  |  | 3 |
| Type II – grained or atomized | C | 4 |
|  |  | 4A |
|  |  | 5 |
|  |  | 5A |
|  |  | 6 |
| Type III - atomized | C | 6 |
|  |  | 7 |
|  |  | 8 |
|  | G | 9 |
|  | H | 10 |

Chemical Characteristics

| Requirement, weight % | Grade A | Grade B | Grade C | Grade G | Grade H |
| --- | --- | --- | --- | --- | --- |
| Aluminum, min | 98.0 | 98.0 | 99.0 | 98.75 | 99.0 |
| Copper, max | 0.50 | 0.50 | 0.50 | - | - |
| Iron, max | 0.50 | 0.50 | 0.50 | 0.55 | 0.20 |
| Silicon, max | 0.50 | 0.50 | 0.50 | 0.25 | - |
| Magnesium, max | 0.10 | 0.10 | 0.10 | - | - |
| Zinc, max | 0.25 | 0.25 | 0.25 | 0.3 | - |
| Nonvolatile matter, min | 99.0 | 99.5 | - | 99.9 | 99.9 |
| Easily extracted fatty and oily matter, max | 1.0 | 1.5 | - | 0.2 | 0.2 |

ALUMINUM POWDER, FLAKED GRAINED, AND ATOMIZED

MIL-DTL-512D

| Classes | Density (g/cm3) | Size ranges mesh (um) | Weight % |
| --- | --- | --- | --- |
| 1 | 0.30 max | +325 mesh (>45) | 1.0 max |
|  |  | -325 mesh (<45) | 99.0 min |
| 2 | No determination | +325 mesh (>45) | 6.0 max |
|  |  | -325 mesh (<45) | 94.0 min |
| 2A | No determination | +100 mesh (>150) | 0.2 max |
|  |  | -100 +200 mesh (150 – 75) | 20.0 max |
|  |  | -200 mesh (<75) | 80.0 min |
| 3 | 0.50 max | +100 mesh (>150) | 0.2 max |
|  |  | -100+200 mesh (150 – 75) | 15.0 max |
|  |  | -200 + 325 mesh (75 – 45) | 15.0 max |
|  |  | -325 mesh (<45) | 80.0 min |
| 4 | 0.90 min | +50 mesh (>300) | 0.0 |
|  |  | -50 + 100 mesh (300 -150) | 3.0 max |
|  |  | -100+200 mesh (150 -75) | 3.0 – 20.0 |
|  |  | -200 mesh (<75) | 80.0 – 97.0 |
| 4A | 0.90 min | +20 mesh (>850) | 2.0 max |
|  |  | -20 + 100 mesh (850 – 150) | 30.0 max |
|  |  | -100 + 200 mesh (150 – 75) | 65.0 max |
|  |  | -200 mesh (<75) | 30.0 – 60.0 |
| 5 | 0.90 min | +12 mesh (>1700) | 0.0 |
|  |  | -12 +30 mesh (1700 – 600) | 13.0 – 26.0 |
|  |  | -30 mesh (<600) | 74.0 – 87.0 |
| 5A | 0.90 min | +30 mesh (>600) | 13.0 – 26.0 |
|  |  | -30 + 50 mesh (600 – 300) | 35.0 – 45.0 |
|  |  | -50 + 140 mesh (300 – 106) | 30.0 – 46.0 |
|  |  | -140 mesh (<106) | 3.0 max |
| 6 | 0.95 – 1.20 | +100 mesh (>150) | 2.0 max |
|  |  | -100 + 200 mesh (150-75) | 20.0 max |
|  |  | -200 + 325 mesh (75 – 45) | 10.0 – 35.0 |
|  |  | -325 mesh (<45) | 65.0 – 90.0 |
| 7 | 0.95 min | +40 mesh (>425) | 0.5 max |
|  |  | -325 mesh (<45) | 25.0 – 50.0 |
| 8 | 0.95 min | +12 mesh (>1700) | 0.5 max |
|  |  | -325 mesh (<45) | 35.0 max |
| 9 | 1.0 min | -200 (<75) | 99.5 min |
|  |  | -325 (<75) | 60.0 min |
| 10 | No determination |