TITANIUM, TECHNICAL: POWDER

MIL-T-13405E

23 February 1984

Superseding

MIL-T-13405D (EA)

25 July 1977

Characteristics

| Type I | Type II |
| --- | --- |
| For use in pyrotechnic mixtures | For use in M36 bomb clusters |

Chemical and physical properties

| Property | Type I | Type II |
| --- | --- | --- |
| Assay (percent Titanium) | 94% min | 96.5% min |
| Burning time | >40 seconds <180 seconds | >90 seconds <220 seconds |
| Particle size | 95% min -75 microns | 95% min -75 microns |
| Mean surface diameter | --- | >3 microns <12 microns |